## Slide 1
Synthesis and catalytic properties of zinc-histidine framework mimicking carbonic anhydrase
Longji Li, Simrat Kaur, Bangbo Yan
Department of Chemistry, Western Kentucky University, Bowling Green, KY 42101
FTIR spectrum of the MOF
Results & Conclusions
Introduction
Materials & Methods
Acknowledgements
Data
Mechanism
Zinc (II) nitrate as a source of zinc
L-histidine as ligand
Solvent – water
KOH – pH regulation
Hydrothermal Method – A process of crystallization – PTFE autoclaves (heated at 120 °C for 72 hours in the oven)
Characterization – Powder X-ray diffraction, thermogravimetric analysis and infrared spectroscopy
Biomimetic Analysis - Hydrolysis of p-NPA
The purpose of this research project was to synthesize, characterize, and analyze a zinc-histidine framework mimicking carbonic anhydrase (CA).
CA is an enzyme that assists rapid interconversion of carbon dioxide and water into carbonic acid, protons, and bicarbonate ions.
Due to CA’s activity, there is a growing interest in using CA for industrial applications such as carbon sequestration and biofuel production. The development of CA is necessary to enhance the efficiency of conversion.
Our product has potential in regulating the atmospheric carbon dioxide level and helping to reduce the greenhouse effect.
TGA spectrum
The FTIR spectrum showed the existence of L-histidine in the framework (amine, cyclic alkene, ester, carboxylic acid, etc.) as well as the Zn-O stretching, confirmed a CA-like crystal structure.
The TGA spectrum showed that the catalyst possesses great thermal stability that there is no significant decrease in mass below 400 ℃. Moreover, the decrease indicated the removal of ligands. In the end, the mass stopped decreasing at 48%, indicating the remaining of the inorganic part.
The catalytic analysis of the decomposition of p-NPA verified the great catalytic ability of the zinc MOF, and the proportional relationship between absorbance and time.
The future research will be focused on the analysis of the crystal structure of the MOF, define the empirical formula of the framework, and testing the performance of CO2 Hydrolysis.
References
Huang, Zhang, et al. A Zinc Coordination Complex Mimicking Carbonic Anhydrase for CO2 Hydrolysis and Sequestration. Inorg. Chem. 2019, 58, 9916-9921.
Catalytic Analysis
X-ray diffraction spectrum
2020 KAS Annual Meeting
N-H stretching 3300-3400 cm-1
-OH stretching 2700-3200 cm-1
C=C stretching 1566-1650 cm-1
Carboxylic acid bending 1395-1440 cm-1
-OH bending 1330-1400 cm-1
Ester stretching 1163-1260 cm-1
Zn-O stretching 518-682 cm-1
Jin, Zhang, et al. Mimic Carbonic Anhydrase Using Metal–Organic Frameworks for CO2 Capture and Conversion. Inorg. Chem. 2018, 57, 4, 2169–2174.